## Slide 1: Edge-TCT with active pixels
Motivation:
  Passive devices enable measurement of charge collection efficiency (CCE), but in-time efficiency is also important for real application
  Smaller signals on pixel edges  larger time walk
  Edge-TCT with active devices allows measurement of time walk dependence on position within pixel
Method:
  Acquisition triggered by laser driver output, adjustment for cable and fibre length, light hits the sample at t=0
  Measure Time of Arrival (ToA) and Time over Threshold (ToT) of the in-pixel comparator output
    ToT – signal size
    ToA – time walk information
  Change signal size by varying laser power
Samples
  RD50-MPW2 W11 (1.9 kOhm cm)
  Unirradiated and 5e14 neutrons (TID 0.5 MRad)
ToA
ToT
laser trig
CabL
light enters sample

## Slide 2: Edge-TCT example
chip surface
depth
Example of CCE and timing measurement
Evaluate average ToT (left) and ToA (right) in a volume 50 μm x 80 μm (W x H), starting 20 μm below surface
ToT = 126 ns
ToA = 9.8 ns

## Slide 3: CCE and timing for different laser power (5e14)
ToT (charge)
ToA (time walk)
Reducing laser power
Reducing laser power
(same z-scale for all measurements)

## Slide 4: Time walk Edge-TCT
5e14
unirrad.
ToT 50 ns
≈ 3500 e-
ToT 50 ns
≈ 3500 e-
Edge-TCT time walk measurement in three different pixels before and after irradiation
Time walk increases with higher threshold (as expected)
Significant pixel-to-pixel variations (manufacturing variations)
Time walk similar before and after irradiation
Measurements in low ToT range limited by noise level

## Slide 5: Time walk – comparison between Edge-TCT and external injection
Cross check – direct charge injection into front-end via 2.8 fF injection capacitance
Both methods in agreement within 1– 2 ns
unirradiated

## Slide 6
Backup

## Slide 7: Edge-TCT measurement setup
Edge-TCT setup by Particulars, spatial resoultion 5 μm
Chip configuration with ZC706 + CaRibou
Analogue COMPOUT signal read out by oscilloscope (DRS 4)

## Slide 8: S-curve (threshold 1000 mV)
unirradiated
5e14 neutron irradiated
Selected three pixels with low, medium and high threshold
No pixel-level Trim-DAC tuning
Baseline 900 mV + Uinj compared to threshold (1000 mV)
beam direction
(≈ 17 e-/mV)

## Slide 9: Time walk – external injection
Charge injected via 2.8 fF injection capacitance – unirradiated sample
Edge-TCT

## Slide 10: Charge – ToT calibration
Calibration (ToT  charge) by charge injection with pulse generator (allows reaching lower Uinj than Car)
  Cinj = 2.8 fF, Thresholds 950 mV and 1000 mV, no TrimDACs
  Measure ToT of COMPOUTBUFF signal on oscilloscope
Pulse Gen.
(Ext. Inj.)
Significant differences in calibration of different pixels
- Apparently due to manufacturing variations

## Slide 11: External injection 5e14
Chart: charge (e)
| 11 | 38 | 56 | 70 | 93 | 112 | 130 | 149 | 180 | 224 | 315
C2R4 1000 mV | 875 | 1750 | 2625 | 3500 | 5250 | 7000 | 8750 | 10500 | 14000 | 17500 | 31500
C2R4 950 mV | 1750 | 1925 | 2100 | 2275 | 2450 | 2625 | 2800 | 2975 | 3150 | 3325 | 3500 | 3850 | 4200 | 4550 | 4900 | 5250 | 5600 | 5950 | 6300 | 6650 | 7000 | 7875 | 8750 | 10500 | 12250 | 14000 | 15750 | 17500 | 31500
C2R3 950 mV | 875 | 1750 | 2625 | 3500 | 5250 | 7000 | 8750 | 10500 | 14000 | 17500 | 31500
C2R3 1000 mV | 1750 | 2625 | 3500 | 5250 | 7000 | 8750 | 10500 | 14000 | 17500 | 31500
C2R1 950 mV | 875 | 1750 | 2625 | 3500 | 5250 | 7000 | 8750 | 10500 | 14000 | 17500 | 31500
C2R1 1000 mV | 1750 | 2625 | 3500 | 5250 | 7000 | 8750 | 10500 | 14000 | 17500 | 31500
simulation | 1000 | 2000 | 3000 | 4000 | 5000 | 6000 | 7000 | 8000 | 9000 | 10000 | 11000 | 12000 | 13000 | 14000 | 15000 | 16000 | 17000 | 18000 | 19000 | 20000 | 21000 | 22000 | 23000 | 24000 | 25000
Significant difference in calibration of different pixels (up to 50 %)
Probed pixels slightly below simulation values
Approx. 5 % difference within pixel between thresholds 50 mV and 100 mV