Material specifications for the production of low mass tapes:

- 25m kapton/25m PU glue/ 50m Al laminate  (GTS  part number 660210) in 305 mm wide roll

or alternative: 50 m kapton/25m PU glue/ 50m Al laminate  (GTS  part number 660220) in 305 mm wide roll

- 25 m adhesive  on release paper (GTS  part number 102100) in 305 mm wide roll

- 25 m adhesive/12.5 m  kapton coverlayer (GTS  part number 322190)

on release foil in 305 mm wide roll

1.Requirements:

1.1. Bare dielectric:

Material: Kapton Dupont type FPC

Appearance: a polyimide film, with an appearance of transparent gold in colour, but uniform within a given roll and from batch to batch.

Thickness: 25 (50) microns  10 %

1.2. Kapton/Al laminate  adhesive:

the adhesive is PU H/T adhesive system

1.3. Al foil:

High ductility aluminum foil

Conductor:        Aluminum  type  Al 1200

The Al foil shall be smooth and free from wrinkles, deep scratches, pits & dents, pinholes, oil and grease contamination or any other defect that may effect life or serviceability of finished laminated product.

1.4.Laminate:

Laminate suitable for flexible printed circuit fabrication

The laminate shall be uniform in appearance and free from adhesive mis-coats, adhesive smear and substantially free from inclusions either within the lamination or wound within the roll.

Peel strength  of Al/kapton should be higher than 0.5N/mm at 1mm/sec pull

All thicknesses  should be  10 % within the specified value

2. Supply & packaging:

Cores: the material shall be supplied on plastic cores.

Length: the minimum roll length will be 50 m

Width: 305  1mm

Identification: The following information shall be supplied with each shipment of material to enable product traceability.

The information shall be attached to the inside of the core on each individual roll of material and attached to the outside of each carton:

- Material part no, Batch No & Roll No

- length and width

- Supplier and Purchaser Order No

- Date of shipment